Appearance 		clear colourless liquid

Viscosity at 25°C, mm2/s		12.500    +/÷  5% tolerance

Specific gravity at 25°C		0,97

Flash point, °C,		320

Fire point DIN 51376 , °C  	390

Pour Point, °C		÷ 50

Boiling Point, °C

Refractive index at 25°C		1,404

Surface tension at 25°C  mN/m            21,1

Vapour tension at 200°C, Pa	1,33

Expansion coefficient  		9,45·10-4

between 25° and 100°C

Specific heat between 25° & 250°C, 	1,50

Thermal conductivity,		0,174

W/m°K (between 25°& 250°C

Viscosity/temperature		0,62

coefficient (1)

Dielectric strength at		18

25°C, kV/mm

Dielectric constant at		2,8

25°C, between 0,5 and 100 kHz

Loss angle tangent at		1·10-4

25°C at 100 kHz

Volume resistivity at		 1·1015

25°C, Ohm · cm

Noac Test	250°C DIN51581	> 1,0 %

(viscosity at       99°C)

(1) Viscosity/temperature coefficient:     1 - (viscosity at 38°C)

Udgave 22.01.2001 rev.SQ-2011-03-15